## Slide 2: Holey SiNx 02
Hole size indicator of the chip Size = N matrix of squares x 5 [um]
This example: Nominal size is 15 (3x5) [um]
Backside C10 (50 um)
Backside C8 (20 um)
Topside C10 (50 um)
Row and column index in binary
So they start at zero (just add 1)
Square: 0
Rectangle: 1
This example:
Row: [2]+1 (010)
Colum: [5]+1 (101)
1 2 3 4 5 6 7 8
1
2
3
4
5
6
7
8
SiNx
SiNx
SiNx surface over Si

## Slide 3: Holey SiNx 02: after PC removal
HSiNx02 C06 (20 um)
1-1
1-8
7-1
8-2
8-8
4-5
5-4
20 um
20 um
20 um
20 um
20 um
20 um
20 um

## Slide 5: Measurements 27.02.2025 thermooptosetup

## Slide 7
Reference at Power 75 uW, 100x1

## Slide 8
Power 25 uW, 100x1

## Slide 9
Power 50 uW, 100x1

## Slide 10
Power 75 uW, 100x1

## Slide 11
Power 100 uW, 100x1

## Slide 12
Power 125 uW, 100x1

## Slide 13
Power 150 uW, 100x1

## Slide 14
Power 175 uW, 100x1

## Slide 15
Power 1 mW, 20x1

## Slide 16
Power 2.5 mW, 10x1

## Slide 17
Power 2.5 mW, 20x1

## Slide 18
Power 2.5 mW, 50x1

## Slide 19
Power 2.5 mW, 100x1, different focus

## Slide 20: Polarization changed to 90 90 90
(45 90 45)

## Slide 21
Power 2.5 mW, 100x1, normal focus

## Slide 22: Polarization changed to 0 90 90
(0 90 45)

## Slide 23
Power 2.5 mW, 100x1, normal focus

## Slide 24: Polarization changed to 90 0 0
(45 0 0)

## Slide 25
Power 2.5 mW, 100x1, normal focus

## Slide 26: 28.02.
Plan new big flake

## Slide 27
Power 2.5 mW, 50x1, focus, 90 0 0 polarization

## Slide 28
Power 2.5 mW, 50x1, focus, 0 0 0 polarization

## Slide 29: Change focus, see signal at two polarizations
new big flake

## Slide 31
Power 2.5 mW, 50x1, focus, 0 0 0 polarization

## Slide 32
Power 2.5 mW, 50x1, focus, 90 0 0 polarization

## Slide 33
Power 2.5 mW, 50x1, focus, 90 90 90 polarization

## Slide 34
Power 2.5 mW, 50x1, focus, 0 90 90 polarization

## Slide 35
Power more than 2.5 mW, 50x1, focus, 0 90 90 polarization

## Slide 36
Power even more than 2.5 mW, 50x1, focus, 0 90 90 polarization

## Slide 37
Power even more than 5 uW, 150x1, focus, 0 90 90 polarization

## Slide 38: 03.03.25

## Slide 39
To check the focus, move slightly in z

## Slide 40: 1. aquire silicon spectrum
Its saved

## Slide 41: On suspended membrane 5 uW

## Slide 42: On flake (1) 2.5 mW

## Slide 43: On flake (2) 2.5 mW

## Slide 44: On flake (3) 2.5 mW

## Slide 45: On flake (4) 0.1 mW, exposure time 150x3

## Slide 46: On flake (5) 1 mW, exposure time 50x3

## Slide 47: Silicon (6) 1 mW, exposure time 50x3

## Slide 48: On flake (7) 1 mW, exposure time 50x3