## Slide 1: Suspension of STO
Jose M. Sojo & Dominik M. Koch
10/02/2025

## Slide 2: FM345 – 35 nm STO over Nb:STO

## Slide 3: Holey SiNx 02
Hole size indicator of the chip Size = N matrix of squares x 5 [um]
This example: Nominal size is 15 (3x5) [um]
Backside C10 (50 um)
Backside C8 (20 um)
Topside C10 (50 um)
Row and column index in binary
So they start at zero (just add 1)
Square: 0
Rectangle: 1
This example:
Row: [2]+1 (010)
Colum: [5]+1 (101)
1 2 3 4 5 6 7 8
1
2
3
4
5
6
7
8
SiNx
SiNx
SiNx surface over Si

## Slide 4: Holey SiNx 02: with PC
HSiNx02 C06 (20 um)
1-1
1-8
7-1
8-2
8-8
20 um
20 um
20 um
20 um
20 um

## Slide 5: Holey SiNx 02: after PC removal
HSiNx02 C06 (20 um)
1-1
1-8
7-1
8-2
8-8
4-5
5-4
20 um
20 um
20 um
20 um
20 um
20 um
20 um